Multichannel Electrochemical workstation

16 Independent channels with following specifications:

- Battery testing voltage range: 0-10V batteries

- Voltage measurement Resolution : 50uV or less

- Applied Current: +/- 100uA to +/- 1.5A with 4-5 ranges between these current range.

- Current resolution: 3 nA or less

- All the  16  channels  require  EIS facility

- EIS freq. Range: 10 mHz to 10KHZ with automated sweep facility for the entire frequency

- Complete battery cycling software facility (Cyclic Voltammetry, Chrono Amperometry, Chrono Potentiometry , Chrono Coulometry, I-V measurment)

- EIS measurement with GEIS, PEIS techniques and analysis.

- Columbic Efficiency factor determination facility

- Columbic efficiency determination facility is required to estimate the lifetime of a battery.

- Facility required to study the phase transformations during the use of the battery.

- Software facility required to predict the lifetime of battery.

- Cell cables (~2.5 meteres) should be provided for all the16 channels.

- Coin cell holders which can be plugged directly to the Instrument should be provided for all the 16channels.

- Desktop  computer  for Instrument control  and Laptop  with i-5 Processor, 4GB RAM, 500 GB HDD, 21’’ Windows 7 Home Basic should be supplied along with the Instrument.

- Minimum warranty must be 2 years.